## Slide 1: Li-Ion Battery Course
Circular Economy
Standard and Regulations
Thermal Design
Battery Ageing
Battery Manage- ment System
Li-Ion Battery Cells
Modelling and Validation
Charging Strategies

## Slide 2: Modelling of Li-Ion Batteries
Learning objectives
Students are familiar with different modeling approaches.
Students get to know the electrical equivalent circuit model and can simulate the transient voltage curve on the cell terminals in response to a current load.
The students know the major types of heat generation in Li-ion cells.
Students are introduced to different methods for model parameterization.
The students implement individual parts of a cell model in Python and compare the simulations with measurements.

## Slide 3: Table of Content
Modelling Approaches
  Physical vs. Equivalent Circuit vs. Blackbox Models
Modelling the electrical behavior
  Level of detail (i.e. model order)
  Parametrization
Modelling the thermal behavior
  Heat generation in Li-Ion cells
Outlook: Modelling battery packs
Literature
Exercises: Implementation of single cell models in Python

## Slide 4: Modelling Approaches
Modelling the cell behavior
Electrochemical model
Equivalent circuit model
Black box model
S. Wang, Battery System Modeling. San Diego: Elsevier, 2021.
Analyzing the reaction mechanisms with partial differential equations
Lumped parameter model simulating the macroscopic physical quantities
Linear of nonlinear function describing the voltage response
Large number of parameters
physically meaningful
Flexible data driven phenomenological model

## Slide 5: 2. Modelling the electrical behavior
Goal of electrical models
Calculate the State of Charge (SoC) as a function of time for a given load profile .
Calculate the voltage across the battery cell terminals at any given time.

## Slide 6: 2. Electrical Equivalent Circuit Model (EECS)
Resistance of current collectors and effects such as ion conductivity in the electrolyte are modelled as a single internal resistance.
All electro-chemical phenomenon are represented by the controlled voltage source, which is dependent on the state of charge, as well as other factors.
+
-

## Slide 7: 2. Parametrization procedures
Continuous Current experiment
Hybrid Pulse Power Characterization (HPPC)
Continuous measurement across the whole SoC range
Low C-Rate (e.g., ) needed for accurate results
Internal resistance can be identified more accurately
Transient behavior of terminal voltage is visible
Accurate measurement of open circuit voltage
Open circuit voltage is measured in discrete steps
Long relaxation phases needed (for accurate results)

## Slide 8: 2. Differential equation (1)
The state variable is the electrical charge stored in the battery cell
or in terms of state of charge

## Slide 9: 2. Output equation
Typically, the voltage on the battery terminals should also be calculated, so the following output equation is required:

## Slide 10: Python exercise 1
Parametrization Take the current and voltage data from a continuous current experiment to determine the open ciricuit voltage and the internal resistance as a function of the state of charge.
Implementation Implement the ordinary differential equation and the output equation in a function, which can be used with the built-in solver from Python (scipy.integrate.solve_ivp package).
Comparison with HPPC data Take the parametrized model and apply a current pulse according to the HPPC. Compare the measured and simulated voltage on the battery terminals.

## Slide 11: 2. Improved internal resistance model
The HPPC reveals transient phenomenon on various time scales, which can be modelled by one or more RC parallel circuits.
+
-

## Slide 12: 2. Differential equation (2)
Equation for a single RC parallel circuits can be derived from Krichhoff’s current law.

## Slide 13: 2. Differential equation (2)
State space representation of the EECS with multiple RC circuits
+
-

## Slide 14: 2. Output equation (2)
State space representation of the EECS with multiple RC circuits
+
-

## Slide 15: 2. Parametrization of detailed EECM
[1] Y. Zheng, Z. Shi, D. Guo, H. Dai, and X. Han, ‘A simplification of the time-domain equivalent circuit model for lithium-ion batteries based on low-frequency electrochemical impedance spectra’, Journal of Power Sources, vol. 489, p. 229505, Mar. 2021, doi: 10.1016/j.jpowsour.2021.229505.
[2] T. Kalogiannis et al., ‘Comparative Study on Parameter Identification Methods for Dual-Polarization Lithium-Ion Equivalent Circuit Model’, Energies, vol. 12, no. 21, p. 4031, Oct. 2019, doi: 10.3390/en12214031.
[1]
[2]

## Slide 16: 2. Parametrization of detailed EECM
Electrochemical Impedance Spectroscopy
T. Kalogiannis et al., ‘Comparative Study on Parameter Identification Methods for Dual-Polarization Lithium-Ion Equivalent Circuit Model’, Energies, vol. 12, no. 21, p. 4031, Oct. 2019, doi: 10.3390/en12214031.
[1]

## Slide 17: Python exercise 2
Implementation of the detailed EECM Implement a Python class for a detailed EECM with a variable number of parallel RC circuits. Formulate the overpotential as a linear state space model.
Comparison with HPPC data Take the parametrized model and apply a current pulse according to the HPPC. Compare the measured and simulated voltage on the battery terminals.

## Slide 18: 3. Modelling the thermal behavior
Goal of thermal models
Calculate the heat flux a function of time for a given load profile . (i.e. the amount of heat generated during a charge / discharge cycle)
Calculate the temperature of the battery cell for a given thermal boundary condition.

## Slide 19: 3. Heat generation mechanisms
: denotes the total heat generation.
: represents reversible heat, reflecting entropic changes during electrochemical reactions.
: represents irreversible heat or joule heat, arising from over- potential, including ohmic losses, charge transfer resistances at the interface, and mass transfer limitations.
: accounts for heat generated by side reactions, indicating phase changes other than crystalline transitions, primarily due to lithium-ion diffusion.
: denotes the heat of mixing, resulting from the formation and relaxation of concentration gradients within the electrolyte.
K. Maher, et. al., ‘Understanding the heat generation mechanisms and the interplay between joule heat and entropy effects as a function of state of charge in lithium-ion batteries’, Journal of Power Sources, vol. 623, p. 235504, Dec. 2024, doi: 10.1016/j.jpowsour.2024.235504.

## Slide 20: 3. Irreversible heat aka joule heat
Charging
Discharging
Electrical power is delivered to the battery terminals (positive current)
The power stored in the battery cell is equal to
Electrical power is released from the battery cell (negative current)
The power delivered to the load is equal to
In both cases the irreversible power loss is equal to

## Slide 21: 3. Irreversible heat aka joule heat
Charging
Discharging
In both cases, the irreversible heat is exothermic (positive sign), which indicates that heat is being generated …
… and released to the surrounding.
… leading to an increase in the temperature of the battery cell.

## Slide 22: 3. Irreversible heat (implementation)
Instead of using the formula to calculate the joule heat, it is favorable break it down into its single components.
Using the state space representation of the EECS with multiple RC circuits introduced earlier, the overpotential is calculated directly.
Hence, the momentary joule heat can be calculated in each time step of the ode-Solver.

## Slide 23: 3. Reversible heat
According to Williford et. al. the rate of heat generated from micro-structural (entropic) changes is equal to
: Temperature in Kelvin
: Entropy change in J/(mole K)
: Faraday constant 96.485 C/mole
: Current in A
R. E. Williford, et. al., ‘Effects of entropy changes in anodes and cathodes on the thermal behavior of lithium ion batteries’, Journal of Power Sources, vol. 189, no. 1, pp. 101–107, Apr. 2009, doi: 10.1016/j.jpowsour.2008.10.078.
Entropic heat coefficient in K/V is a function of the state of charge

## Slide 24: 3. EHC from potentiometric method
The entropic heat coefficient (EHC) can be measured for various SoCs as a change in open-circuit voltage as a function of temperature.
Z. Geng, et. al., ‘A Time- and Cost-Effective Method for Entropic Coefficient Determination of a Large Commercial Battery Cell’, IEEE Trans. Transp. Electrific., vol. 6, no. 1, pp. 257–266, Mar. 2020, doi: 10.1109/TTE.2020.2971454.

## Slide 25: 3. EHC from heat flux measurements
Battery cell with actively controlled surface temperature
Precise heat flux measurement on the surface
Charge / discharge current pulses with varying amplitude but constant electric charge
R. Christen, et. al., ‘New Experimental Approach for the Determination of the Heat Generation in a Li-Ion Battery Cell’, Energies, vol. 14, no. 21, p. 6972, Oct. 2021, doi: 10.3390/en14216972.

## Slide 26: Python exercise 3
Implementation of heat generation Given the EHC as a function of the SoC. Supplement the existing detailed EECM with a heat generation term that considers the irreversible and reversible effects.
Simulation of heat generation Calculate the instantaneous heat flow for a given current profile and plot it. Also determine the total amount of heat generated during the load cycle.

## Slide 27: 3. Thermal equivalent circuit model
[1] A. Broatch, P. Olmeda, X. Margot, and L. Agizza, ‘A generalized methodology for lithium-ion cells characterization and lumped electro-thermal modelling’, Applied Thermal Engineering, vol. 217, p. 119174, Nov. 2022, doi: 10.1016/j.applthermaleng.2022.119174.
[2] R. Rizk, H. Louahlia, H. Gualous, and P. Schaetzel, ‘Experimental analysis and transient thermal modelling of a high capacity prismatic lithium-ion battery’, International Communications in Heat and Mass Transfer, vol. 94, pp. 115–125, May 2018, doi: 10.1016/j.icheatmasstransfer.2018.03.018.
[1]
[2]
Concentrated heat capacity with thermal conductivity paths to the environment utilizing all existing symmetries.
Usually, the spatial temperature resolution is limited to the differentiation between core and surface temperature.

## Slide 28: 3. Thermal properties
Heat capacity
Thermal conductivity
The specific heat capacity is a material property.
The heat capacity of a given component is calculated in accordance with:
The heat capacity has the unit
The thermal conductivity is a material property.
The thermal conductance of a given component is calculated in accordance with:
The thermal conductance has the unit

## Slide 29: 3. Thermal equivalent circuit model
Single heat storage element (with )
Discretization with multiple heat storage elements
=
=

## Slide 30: Literature
S. Wang, Battery System Modeling. San Diego: Elsevier, 2021.
G. L. Plett, Battery management systems: Volume 1: battery modeling. in Artech House power engineering and power electronics. Boston London: Artech House, 2015.